## Slide 1: RPD 135 National Airport Pavement & Materials Research Center (NAPMRC)

## Slide 2: High Temperature Pavement Test Facility- RPD 135
Contract Funds ($K)
Projects | FY15 | FY16 | FY17
Maintenance and Equipment | 50 | 100 | 100
Set-up Database, Process and Analyze Data | 150 | 200 | 400
Test Pavement Construction | 200 | 300 | 300
Data Acquisition System & Instrumentation | 50 | 200 | 100
APTV Operation / Warranty | 300 | 0 | 450
TOTAL | $ 750 | $ 800 | $ 1350

## Slide 3: APTV/HVS-A

## Slide 4: HVS-A Test Pavement

## Slide 5: HVS-A Acceptance Test Strips

## Slide 6: HVS-A Acceptance Test Strips
PAVEMENT CROSS-SECTION

## Slide 7: HVS-A Acceptance Test Strips

## Slide 8: HVS-A TS: Response and Traffic Tests

## Slide 9: HVS-A ACCEPTANCE TEST STRIPS
Objectives:
Study the effects of Tire Pressure on
performance of HMA layer.
Tests:
Response Tests.
Traffic Tests.

## Slide 10: HVS-A TS: TRAFFIC TESTS
Tire pressure: 210-psi Test Strip-1
254-psi Test Strip-2
Pavement Temperature: 120 deg. F measured at a depth of 1-inch below pavement surface.
Test Speed: 2-mph
Wheel loads: 61,300-lbs.
Failure Criterion: 1-inch surface rut

## Slide 11: HVS-A TS: Wander Pattern

## Slide 12: HVS-A TS: Response and Traffic Tests

## Slide 13: HVS-A TS: Traffic Tests

## Slide 14: HVS-A TS: Traffic Tests

## Slide 15: HVS-A TS: Traffic Tests

## Slide 16: HVS-A TS: Traffic Tests
Comparison of Surface Profiles at
Failure Criterion (1-in. rut)

## Slide 17: HVS-A TS: Traffic Tests
Comparison of Surface Profiles at
2400 passes

## Slide 18
TEST STRIP-2: Wheel Load - 61,300 lbs; Tire Pressure - 254-psi

## Slide 19
TEST STRIP-2: Wheel Load - 61,300 lbs; Tire Pressure - 254-psi

## Slide 21: Future Research
EVALUATION OF NEW ASPHALT TECHNOLOGIES FOR AIRFIELD PAVEMENTS
Warm Mix Asphalt, Stone Matrix Asphalt, Polymer Modified Binders,
RAP Mixes, Full-Depth Rehabilitation
PROBLEM: Lack of Guidance/Standards/Specifications
Lack of Performance Data
Laboratory Performance Evaluation
Full-Scale APT
NAPMRC
Field Performance Evaluation
Evaluate:
Rutting
Fatigue
Moisture Susceptibility
Durability
Low Temperature Cracking
Full-Scale APT:
Rutting
Fatigue
Tire Pressure Effects
WMA
RAP/RAS
Full Depth Reclamation
Compare to P-401 HMA
Field Projects:
Lab Evaluation of Field Mixes
Construction Evaluation
Evaluate:
Mix Design Production, Construction
Support from AAS-100, ADO

## Slide 22
Objectives, Pavement
Construction, Sensors
NDT & Pavement
Characterization
Full-Scale APT,
Pavement Evaluation
Posttraffic Testing
TEST CYCLE (TC) AT NAPMRC

## Slide 23
PG
64-22
PG
64-22
PG
76-22
PG
76-22
PG
76-22
PG
76-22
P401
HMA
WMA
P401
HMA
P401
HMA
WMA
WMA
214
psi
214
psi
214
psi
214
psi
214
psi
214
psi
254
psi
254
psi
254
psi
254
psi
254
psi
254
psi
MATERIAL
TIRE
PRESSURE
BINDER
TYPE
NAPMRC
Test Cycle-1
(TC-1)

## Slide 24: Pavement Cross Sections

## Slide 25
PG
76-22
PG
76-22
PG
64-22
PG
76-22
PG
76-22
PG
76-22
RAP
1
RAP
2
WMA
1
P401
HMA
WMA
3
WMA
2
ALL TESTS at
:254 psi tire pressure
: 70,000 lbs wheel load
MATERIAL
BINDER
TYPE
CRACKING
(test during
winter)
RUTTING
(test at high
temperature)
NAPMRC
Proposed
Test Cycle-2
(TC-2)

## Slide 26: Future Research
Use of Additives and Nanoparticles to Improve Performance of Airport Pavement Materials
Evaluate the use of Additives and Nanoparticles for Improved Performance of Airport Pavement Materials
Develop Standards/Specifications and Guidelines for Pavement Materials that have been modified with Nanoparticles and other Additives.
LITERATURE REVIEW CURRENTLY UNDERWAY