## Slide 1: RPD-137 Field Instrumentation and Testing

## Slide 2: Field Instrumentation and Testing (RPD 137)
Contract Funds ($K)

## Slide 3: RPD – 137
Field Instrumentation projects –
  Continue data collection and analysis from
    LaGuardia International Airport, New York City, NY
    JFK Intl. Airport, New York City, NY
    EWR Intl. Airport, Newark, NJ

## Slide 4: Current FAA Airport Instrumentation Projects
LaGuardia Airport, NYC – AC Overlay Pavement
JFK International Airport, NYC – PCC Pavement
Newark Liberty International Airport, Newark – AC Overlay Pavement
Baltimore Washington International Airport, Baltimore

## Slide 5
Study slippage failures on Runway 4R-22L at EWR.

## Slide 7: Installation of Asphalt Strain Gages
Base layer strain gages are embedded in the milled surface
Overlay gages are placed on top of the milled surface
All wires are connected in lighting cans

## Slide 9: Newark Strain Gage Installation Location
High-Speed Taxiway N of Newark Liberty International Airport

## Slide 10: Strain Gage Layout at EWR

## Slide 12: Cataloguing Transverse Strain Gage Responses
Transverse Dual Wheel (wheel away from gage pair, no delamination evidence)
Transverse Dual Tandem (wheel away from gage pair, no delamination evidence)
Tension Compression
Tension Compression

## Slide 13: Delamination Evidence in Strain Responses
Early indications: large discrepancy between responses but no inversion.
  Can be a clue that delamination is starting to occur, but is not analyzed as delamination evidence.
Delamination evidence: bottom of overlay gage in tension (A), top of base layer gage in compression (B), very high ΔStrain value.
Overlay
Base Layer
Overlay
Base Layer
Tension Compression
Tension Compression

## Slide 14: Progression of Delamination: LSG-6
Top left: July 10th, 2013
Top right: July 18th, 2013
Bottom right: July 7th, 2014
Overlay
Base Layer
Overlay
Base Layer
Overlay
Base Layer
No Delamination
Early Indications
Delamination
Tension Compression
Tension Compression
Tension Compression

## Slide 15
Courtesy of PANYNJ 2014

## Slide 16: Transverse ASG Responses with No Delamination Evidence
Correlation = 0.92
 Compression Tension 
 Compression Tension 

## Slide 17: Longitudinal ASG Responses with No Delamination Evidence
 Compression Tension 
 Compression Tension 

## Slide 18: Transverse ASG Responses with Delamination Evidence
 Compression Tension 
 Compression Tension 

## Slide 19: Longitudinal ASG Responses with Delamination Evidence
 Compression Tension 
 Compression Tension 

## Slide 20
JFK Runway 13R-31L Reconstruction Project
Taxiway-Z
4,443 m long, 61 m wide
Completed in 2 phases

## Slide 21: PROJECT SPECIFIC OBJECTIVES
Study curling in slabs (wet-freeze climatic region)
Measure total strain and load induced strain in slabs under multi-gear aircraft such as A-380, B-777, B-747, etc.
Measure load induced strain at an offset under multi-gear aircraft such as A-380, B-777, B-747, etc.

## Slide 22: RUNWAY 13R-31L RECONSTRUCTION PROJECT

## Slide 23: SENSOR LAYOUT
Slab Size: 7.62 m x 7.62 m
48 strain gages
10 Pressure Cells
Temperature Gages

## Slide 26
31  (T)
23  (T)
28  (T)

## Slide 27: RUNWAY 4L-22R RECONSTRUCTION PROJECT
PCC Slab Thickness using
FAA Standard Flexural Strength (700 psi)
PCC Slab Thickness using 950 psi
(Mean – 1 Std. Dev.) Flexural Strength

## Slide 28
JFK Runway 4L-22R RSA Compliance/Runway
Reconstruction Project
Taxiway-J
2015
Taxiway-Z Instrumented
In 2010