## Slide 1: Full-Scale Testing – Perpetual Pavement Update

## Slide 2
CONSTRUCTION CYCLE – 7 (CC-7)
PRIMARY OBJECTIVES
  Develop Perpetual Pavements Design criterion for airport pavements.
  Vertical strain threshold in the intermediate HMA layer to limit rutting.
  Horizontal strain threshold in the HMA base layer to prevent bottom-up fatigue cracking.
  Relationship between laboratory fatigue strain threshold and measured field HMA strains.
  Study strain distribution in the HMA layer.

## Slide 3
CONSTRUCTION CYCLE – 7 (CC-7)
PRIMARY OBJECTIVES
  Verify/Refine/Modify fatigue model based on the ratio of dissipated energy change (RDEC)
  Overload (South Side Pavements)
  Determine allowable aircraft overload criteria for flexible pavement.

## Slide 4
CC7 – PERPETUAL PAVEMENTS

## Slide 5: Pavement Cross Sections

## Slide 6: Traffic Tests:
Standard NAPTF wander pattern.
55 kips wheel load, 6-wheel gear.
Pavement Monitoring
  Straight Edge Rut Depth Measurements
  Surface profiles
  Crack maps

## Slide 7
Vertical strains measured in HMA layer

## Slide 8
Transverse strains measured at HMA Surface

## Slide 9
Transverse strains measured at Bottom of HMA

## Slide 12: Summary:
Two of the thicker perpetual pavement test sections (LFP-1N and LFP-2N) did not show any evidence of fatigue cracks, whereas LFP-3N and LFP-4N showed severe fatigue cracking.
All the cracks were found to be top-down cracks. The conventional flexible pavement test section LFC-5N showed severe rutting and fatigue cracking.
The test section performance shows that under given aircraft gear loading used in the study, by increasing HMA thickness from 10 in. to 12 in. fatigue cracking was eliminated during the duration of testing (almost 38,000 passes).

## Slide 13: Summary:
FOSP strain measurements were useful in understanding the HMA layer behavior.
Laboratory fatigue tests are under progress to determine input properties for the fatigue model incorporated in FAARFIELD and comparison will be made between predicted and observed fatigue life.
Posttraffic trenching – after completion of CC7 Overload study.

## Slide 14
Thank you!