## Slide 1: RPA - P2 NAPMRC (National Airport Pavement & Materials Research Center)

## Slide 2: RPA P2 Overview - NAPMRC
FY 2016 Accomplishments
Research Goals
Funding Requirements
Research Goals
More durable, long-lived airport pavements, reduced lifecycle costs, better prediction of pavement service life, and accurate assessment of aircraft-pavement compatibility
Standards/specification for new asphalt technologies such as WMA, SMA, RAP, etc.
Deliverables
Technical Reports, technical papers.
Complete traffic tests on Test Cycle – 1 (TC-1) by end of FY2016.
Lab study on SMA & RAP completed.
Milestones
- Complete tests on HMA at 214-psi tire pressure √
- Complete tests on WMA at 214-psi tire pressure √
- Complete tests on HMA at 254-psi tire pressure √
- Complete tests on WMA at 254-psi tire pressure √
- Indoor Lanes (2) remaining.
NAPMRC FY 2016 through FY 2018.
Need
NAPMRC provides the ability to test the surface layers, pavement materials, and alternative pavement materials. Improved paving materials characterization will conserve airport development funds and reduce the downtime of runways from construction and maintenance activities. Test results will help in developing standards/specification for new asphalt technologies such as WMA, SMA, RAP, etc.
 | FY 2016 | FY 2017 | FY-18
Funding Target ($000) | $800 | $1700 | $1751
P2.1: Pavement Construction | - | $400 | $400
P2.2: Facility Operation | $800 | $1,100 | $1,100
P2.3: Facility Maintenance | - | $200 | $251

## Slide 3: Aircraft Tire Pressure Trends
Old X Category Limit
New X Category Limit
Tire Pressure, bar

## Slide 4: Aircraft Gross Weight Trends
[Published by the International Industry Working Group (IIWG), 2010]
73,300 lbs
A350-900
HVS-A
100,000 lbs

## Slide 8
Objectives, Pavement
Construction, Sensors
NDT & Pavement
Characterization
Full-Scale APT,
Pavement Evaluation
Posttraffic Testing
TEST CYCLE (TC) AT NAPMRC

## Slide 9
PG
64-22
PG
76-22
PG
76-22
PG
76-22
PG
64-22
PG
76-22
P401
HMA
WMA
P401
HMA
P401
HMA
WMA
WMA
210
psi
210
psi
210
psi
210
psi
210
psi
210
psi
254
psi
254
psi
254
psi
254
psi
254
psi
254
psi
MATERIAL
TIRE
PRESSURE
BINDER
TYPE
NAPMRC
Test Cycle-1
(TC-1)

## Slide 10: Pavement Cross Sections

## Slide 12
PG
64-22
PG
76-22
PG
76-22
PG
76-22
PG
64-22
PG
76-22
P401
HMA
WMA
P401
HMA
P401
HMA
WMA
WMA
210
psi
210
psi
210
psi
210
psi
210
psi
210
psi
254
psi
254
psi
254
psi
254
psi
254
psi
254
psi
NAPMRC
Test Cycle-1
(TC-1)
Testing Completed
Currently Testing
CENTER
SECTIONS
254-psi 90F

## Slide 19
NAPMRC TC1 TEST PAVEMENT PERFORMANCE |  |  |  |  |  |  |  |  | 
 | Pavement Temperature = 120 deg.F |  |  |  | Pavement Temperature = 90 deg.F |  |  |  | 
Material | Binder | Tire Pressure, psi | Passes to Failure |  | Binder |  | Tire Pressure, psi | Passes to Failure | 
P401 HMA | PG64-22 | 210 | 220 |  | PG64-22 |  | 210 |  | 
 |  | 254 | 130 |  |  |  | 254 | 2600 | 
 | PG76-22 | 210 | 620 |  | PG76-22 |  | 210 |  | 
 |  | 254 | 700 |  |  |  | 254 | 0.64 in Rut @ 5022 | 
WMA | PG64-22 | 210 | 220 |  | PG64-22 |  | 210 |  | 
 |  | 254 | 140 |  |  |  | 254 | 2600 | 
 | PG76-22 | 210 | 800 |  | PG76-22 |  | 210 |  | 
 |  | 254 | 520 |  |  |  | 254 | Testing in Progress | 
(Preliminary test results)

## Slide 20
No. of Passes to Failure: 800
Traffic Tests Terminated: 3906
No. of Passes to Failure: 220
Traffic Tests Terminated: 930
No. of Passes to Failure: 600
Traffic Tests Terminated: 3534
No. of Passes to Failure: 220
Traffic Tests Terminated: 992
NAPMRC-TC1 SOUTH TEST AREA

## Slide 21
LABORATORY CHARACTERIZATION

## Slide 22: Laboratory Characterization
Asphalt Mixtures:
  Dynamic Modulus Test
  Repeated Creep-Recovery Tests at Variable Stress Levels
  Repeated Creep-Recovery Tests at Variable Rest Periods
Asphalt Binders:
    Multiple Stress Creep-Recovery (MSCR)
Granular Materials:
  Resilient Modulus Test
  Repeated Creep-Recovery
  Triaxial Test to Calibrate CAP Model

## Slide 23: Modelling – Texas A&M University
Development of Beta Version of Standalone PANDA-AP
Implementation of a robust constitutive relationship for granular layers
Conduct lab experiments on NAPMRC HVS-A materials
Conduct Performance Simulations

## Slide 24: Modelling – Texas A&M University
Standalone PANDA-AP:
Considers failure mechanisms
Can be used as a supplement to FAARFIELD for refined analysis
Allows for the definition of different gear configurations, loading type, and pavement structure
User-friendly and customized for airfield pavements
Will be free to public and Independent of commercial FE software, such as Abaqus and Ansys

## Slide 25: Modelling – Texas A&M University
PANDA Enhancement for Sub-layers:
Incorporates failure mechanisms for sub-layers
Accounts for permanent deformation of base, sub-base, and subgrade
Considers permanent deformation both due to shearing and densification
Can be applied for performance prediction of relatively thin AC pavements

## Slide 26: Modelling – Texas A&M University
Performance Simulations:
Create 2D and 3D FE representation of airfield pavements subjected to different gear configurations
Analyze available lab experiments on FAA previous NAPTF materials
Conduct performance simulations of NAPTF sites to further validate and refine PANDA-AP
  Compare field rutting of NAPTF-CC3 sections with FE simulations

## Slide 27: Other Research
Completed:
Laboratory Study on Stone Matrix Asphalt [Rutgers University]
HMA mixes with RAP [Univ. of California, Davis]

## Slide 28: SMA Study
AAPTP 04-04 (Prowell et al., 2009) developed initial recommendations for SMA use on airfields
Study to utilize recommended specs to design two SMA mixtures
    9.5mm and 12.5mm NMAS
Compare to performance of two P401 mixtures using identical aggregate sources
    15% natural sand and 0% natural sand

## Slide 29: SMA Study
Performance
Mixture stiffness
  P401 and SMA mixtures similar
  SMA showed slightly less stiffness at higher temperatures; most likely due to higher asphalt contents
Rutting Resistance
  P401 showed most rut resistance (lowest asphalt content)
  P401 with 15% natural sand most rut potential (rounded aggregate = poor shear strength)
  Both SMA mixtures met FAA APA specification

## Slide 30: SMA Study
Performance
Fatigue cracking
  Both SMA mixtures showed better fatigue resistance than P401
  Crack initiation and crack propagation
  Higher effective asphalt contents

## Slide 31
PG
76-22
PG
76-22
PG
64-22
PG
64-22
PG
76-22
PG
76-22
RAP
1
RAP
2
WMA
1
P401
HMA
WMA
3
WMA
2
MATERIAL
BINDER
TYPE
CRACKING
(test during
winter)
RUTTING
(test at high
temperature)
NAPMRC
Proposed
Test Cycle-2
(TC-2)

## Slide 32: Future Research
EVALUATION OF NEW ASPHALT TECHNOLOGIES FOR AIRFIELD PAVEMENTS
Warm Mix Asphalt, Stone Matrix Asphalt, Polymer Modified Binders,
RAP Mixes, Full-Depth Rehabilitation
PROBLEM: Lack of Guidance/Standards/Specifications
Lack of Performance Data
Laboratory Performance Evaluation
Full-Scale APT
NAPMRC
Field Performance Evaluation
Evaluate:
Rutting
Fatigue
Moisture Susceptibility
Durability
Low Temperature Cracking
Full-Scale APT:
Rutting
Fatigue
Tire Pressure Effects
WMA
RAP/RAS
Full Depth Reclamation
Compare to P-401 HMA
Field Projects:
Lab Evaluation of Field Mixes
Construction Evaluation
Evaluate:
Mix Design Production, Construction
Support from AAS-100, ADO