## Slide 1: RPA - P2 NAPMRC (National Airport Pavement & Materials Research Center)

## Slide 2: RPA P2 Overview - NAPMRC
FY 2016-2017 Accomplishments
Research Goals
Funding Requirements
Research Goals
More durable, long-lived airport pavements, reduced lifecycle costs, better prediction of pavement service life, and accurate assessment of aircraft-pavement compatibility
Standards/specification for new asphalt technologies such as WMA, SMA, RAP, etc.
Deliverables
Technical Reports, technical papers.
Complete traffic tests on Test Cycle – 1 (TC-1) by end of FY2016.
Lab study on SMA & RAP completed. √
Milestones
- Complete tests on HMA at 210-psi tire pressure √
- Complete tests on WMA at 210-psi tire pressure √
- Complete tests on HMA at 254-psi tire pressure √
- Complete tests on WMA at 254-psi tire pressure √
- Indoor and Outdoor Lanes √
NAPMRC FY 2017 through FY 2019.
Need
NAPMRC provides the ability to test the surface layers, pavement materials, and alternative pavement materials. Improved paving materials characterization will conserve airport development funds and reduce the downtime of runways from construction and maintenance activities. Test results will help in developing standards/specification for new asphalt technologies such as WMA, SMA, RAP, etc.
 | FY 2017 | FY 2018 | FY-19
Funding Target ($000) | $1,700 | $1,530 | $1,620
P2.1: Pavement Construction | $400 | $360 | $270
P2.2: Facility Operation | $1,100 | $950 | $1,010
P2.3: Facility Maintenance | $200 | $220 | $340

## Slide 3
NAPTF
NAPMRC
Material Processing
Facility
Material Testing
Laboratory

## Slide 6
Objectives, Pavement
Construction, Sensors
NDT & Pavement
Characterization
Full-Scale APT,
Pavement Evaluation
Posttraffic Testing
TEST CYCLE (TC) AT NAPMRC
CURRENTLY UNDER
PROGRESS

## Slide 7
PG
64-22
PG
76-22
PG
76-22
PG
76-22
PG
64-22
PG
76-22
P401
HMA
WMA
P401
HMA
P401
HMA
WMA
WMA
210
psi
210
psi
210
psi
210
psi
210
psi
210
psi
254
psi
254
psi
254
psi
254
psi
254
psi
254
psi
MATERIAL
TIRE
PRESSURE
BINDER
TYPE
NAPMRC
Test Cycle-1
(TC-1)

## Slide 8: Pavement Cross Sections

## Slide 9: Test Parameters – Response Tests
Lateral Wander Positions
Tire pressure to 210-psi for tests on South.
Pavement Temperature: 120 deg. F measured at a depth of 2-inch below pavement surface.
Test Speed: 3-mph
Loading Gear: Single Wheel
Apply 22 passes at wheel loads of 20-kips, 30-kips, and 40-kips respectively.

## Slide 10: Test Parameters – Traffic Tests
Pavement Temperature: 120 deg. F measured at a depth of 2-inch below pavement surface.
Test Speed: 3-mph

## Slide 11
PG
64-22
PG
76-22
PG
76-22
PG
76-22
PG
64-22
PG
76-22
P401
HMA
WMA
P401
HMA
P401
HMA
WMA
WMA
210
psi
210
psi
210
psi
210
psi
210
psi
210
psi
254
psi
254
psi
254
psi
254
psi
254
psi
254
psi
NAPMRC
Test Cycle-1
(TC-1)
Testing Completed
CENTER
SECTIONS
254-psi 90F

## Slide 12
Preliminary Test Results

## Slide 13
No. of Passes to Failure: 800
Traffic Tests Terminated: 3906
No. of Passes to Failure: 220
Traffic Tests Terminated: 930
No. of Passes to Failure: 600
Traffic Tests Terminated: 3534
No. of Passes to Failure: 220
Traffic Tests Terminated: 992
NAPMRC-TC1 SOUTH TEST AREA (210-psi; 120F)

## Slide 14
NAPMRC-TC1 NORTH TEST AREA (254-psi; 120F)

## Slide 15
NAPMRC-TC1 CENTER TEST AREA (254-psi; 90F)

## Slide 16
LABORATORY CHARACTERIZATION

## Slide 17: Laboratory Characterization
Asphalt Mixtures:
  Dynamic Modulus Test
  Repeated Creep-Recovery Tests at Variable Stress Levels
  Repeated Creep-Recovery Tests at Variable Rest Periods
Asphalt Binders:
    Multiple Stress Creep-Recovery (MSCR)
Granular Materials:
  Resilient Modulus Test
  Repeated Creep-Recovery
  Triaxial Test to Calibrate CAP Model

## Slide 18
PG
76-22
PG
76-22
PG
64-22
PG
64-22
PG
76-22
PG
76-22
RAP
1
RAP
2
WMA
1
P401
HMA
WMA
3
WMA
2
MATERIAL
CRACKING
(test during
winter)
RUTTING
(test at high
temperature)
NAPMRC
Test Cycle-2
(TC-2)
Tire Pressure
254 psi

## Slide 19: Pavement Cross Sections
SANDY SUBGRADE
CBR 15
NAPMRC TC-2 PAVEMENT CROSS SECTION
P-401 HMA/WMA SURFACE
9 inches
P-209 CRUSHED STONE BASE
8 inches
P-154 SUBBASE
12 inches

## Slide 20: Future Research
EVALUATION OF NEW ASPHALT TECHNOLOGIES FOR AIRFIELD PAVEMENTS
Warm Mix Asphalt, Stone Matrix Asphalt, Polymer Modified Binders,
RAP Mixes, Full-Depth Rehabilitation
PROBLEM: Lack of Guidance/Standards/Specifications
Lack of Performance Data
Laboratory Performance Evaluation
Full-Scale APT
NAPMRC
Field Performance Evaluation
Evaluate:
Rutting
Fatigue
Moisture Susceptibility
Durability
Low Temperature Cracking
Full-Scale APT:
Rutting
Fatigue
Tire Pressure Effects
WMA
RAP/RAS
Full Depth Reclamation
Compare to P-401 HMA
Field Projects:
Lab Evaluation of Field Mixes
Construction Evaluation
Evaluate:
Mix Design Production, Construction
Support from AAS-100, ADO